SysMetEx - Standard Operating Procedures

Bioleaching Experiments (LNU)

Procedure:

- 250 ml Erlenmeyer flasks

- Volume: 100 ml

- Temperature: 40 °C

- Aeration: none

- Shaking speed: 150 rpm

- Medium: Mackintosh medium (MAC)

- Mineral content: 2 %

- Mineral grain size: 50-100 µm

- Starting pH: ~1.8

- Inoculation: 1 x 107 cells per ml per species

- Endpoint: ORP > 400 mV (Ag/AgCl) + 14 days

- Metadata: pH, Redox potential (Ag/AgCl), copper, total iron, soluble iron, elemental sulfur, total soluble sulfur

- RNA/Prot Sampling: at endpoint, planktonic and mineral pellets for UL